## Slide 1: US Air Force Model Defender Belt System
Lightweight
Flame Resistant
MOLLE
Compatible
Lifetime Warranty
Specifications are approximate and subject to change without notice. ©2024 Blue Force Gear, Inc. All Rights Reserved.
877.430.2583
Cage Code: 3X9S8
DUNS Number: 152028291
Sales@BlueForceGear.com
166 Pine Barren Rd., Pooler, GA 31322
Blue Force Gear has developed several load carriage products built specifically for the US Air Force Security Forces Squadron Defender’s mission profile. Outlined below are the items included in the Blue Force Gear and the salient characteristics of each item.
BELT SPECIFICATIONS: MFG: Blue Force Gear Fully Integrates with any MOLLE compatible accessories. Quality and performance beyond military grade. 3 rows of MOLLEminus slots to accommodate accessories Inner layer comprised of a stiffener made of a 12-layer composite material COBRA buckle Fully adjustable for comfortable fit Made in the USA. | COMPOSITE MATERIAL SPECIFICATIONS: Made in the USA. 0.03” thick (0.762mm) Polymer coated composite material (ASTM D-1777) Bonded fabric composite with strong peel adhesion of no more than 25 lbs/in (ASTM D-751) Enhanced abrasion resistance – over 3000 cycles on Taber abrasion (ASTM D-3884) Water resistant - Dynamic Absorption value of no more than 7% of its own weight (AATCC 70) Flexible and lightweight – Weighs less than 25 oz/yd (ASTM D-3776) High tensile strength – Over 500 ft.lbs. tear strength (ASTM D-5034 Grab) Flame Resistant - 3.7 second 1.5” char (Fed Std. 191A, Method 5903) Impact Resistant - superior impact resistance over typical thermoplastic composites, maintaining this performance advantage even at -40°C. Recyclable - The 100% PP composition is fully recyclable with polypropylene recycle streams.
DETAILED LIST OF AVAILABLE SYSTEM ACCESSORIES:
Individual Belt w/COBRA Buckle. Complete w/ 1.5” Inner or 2” Inner Belt:
GRID PRO TACTlCAL BELT (1X) | PN: BELT-GRID-02-XX-MC | Weight: <10 oz
AFD SINGLE M4 MAG POUCH (3X) | PN: HW-AFD-M4-1-MC | Weight: 50g AFD DOUBLE M4 MAG POUCH (1X) | PN: HW-AFD-M4-2-MC | Weight: 89g AFD TRIPLE M4 MAG POUCH (1X) | PN: HW-AFD-M4-3-MC | Weight: 124g AFD SIX M4 MAG POUCH (1X) | PN: HW-AFD-M4-6-MC | Weight: 181g
DOUBLE PISTOL MAG POUCH (2X) | PN: HW-M-PISTOL-2-BG-MC | Weight: 50g
SINGLE PISTOL MAG POUCH (1X) | PN: HW-M-PISTOL-1-BG-MC | Weight: 25g
LOW PROFILE GP POUCH (1X) | PN: HW-AFD-UPZ-06-MC | Weight: 132g
AFD DOUBLE CUFF POUCH (1X) | PN: HW-AFD-CUFF-MC | Weight: 45g
BATON POUCH (1X) | PN: HW-TSP-BATON-01-MC | Weight: 24g
AFD Flashlight Pouch (1X) | PN: HW-AFD-FLASHLIGHT-MC | Weight: 24g
ULTRALIGHT DUMP POUCH (1X) | PN: HW-M-DP-S-MC | Weight: 61g
HOLSTER ADAPTER (1X) | PN: HANGER-HOLSTER-01 | Weight: 91g
PN: K-SP-AFD-01